## Slide 1: RAS Research Update and Best Practices
Dr. J. Richard Willis
Alabama Asphalt Pavement Association Meeting
March 9, 2016
Notes: Challenge in the industry today!

## Slide 2: RAS History
First considered in the early 1980s
Research completed on Manufacturer’s Waste RAS
Preliminary specs in 1990s
Today: 11 million tons of shingles/yearly
  10 million Post-Consumer
  1 million Manufacturer’s Waste

## Slide 3: It’s a Different Animal

## Slide 4: Things to Consider
RAP
RAS
3 – 6 % asphalt binder
94 – 97% stone
19 – 36% asphalt
2 – 15% fibers
20 – 38% mineral aggregate
8 – 40% mineral filler

## Slide 5: RAS Binder Challenges
Lack of guidance on characterizing RAS binders
Many DSRs cannot test high temperature grade due to water boiling
Challenge with BBR testing
  Binder does not relax
Notes: Changed Most to Many

## Slide 6: RAS Binder Characterization Needs
What is the variability of high and low temperature characterization?
Can I extrapolate the high temperature grades?
How can I determine low temperature grades of binder?

## Slide 7: Materials Used
Manufacturer’s Waste
  Michigan, Texas, New Hampshire
Post-Consumer
  Oregon, Michigan, Georgia

## Slide 8: Methodology
Completed 3 extractions of each RAS binder
Run following methodology three times on each extraction
  Tested binder properties at 82, 88, and 94°C
  Determine critical high temperature grade through extrapolation
  Measure critical high temperature grade

## Slide 10: Measured vs Extrapolated
Dataset | Measured Data, °T |  | Extrapolated Data, °T |  | p-value
 | Average | Variance | Average | Variance | 
All Data | 147.5 | 150.4 | 146.2 | 626.1 | 0.73
Michigan MW | 137.7 | 30.6 | 132.9 | 19.1 | 0.06
Michigan TO | 155.4 | 69.2 | 167.8 | 1090.4 | 0.30
Oregon | 147.2 | 21.5 | 144.3 | 26.4 | 0.22
New Hampshire | 156.3 | 75.3 | 144.9 | 172.9 | 0.04
Georgia | 156.5 | 144.8 | 157.7 | 1641.3 | 0.93
Texas | 131.9 | 25.0 | 129.7 | 12.0 | 0.29
Post-Consumer | 147.9 | 184.5 | 147.5 | 647.4 | 0.94
Manufacturer’s Waste | 147.2 | 122.0 | 145.0 | 625.7 | 0.68
t-Test with unequal variances
Α = 5%
Ho: Measured = Extrapolated

## Slide 11: How Much Binder is in the RAS?
Chemical extraction vs. Ignition Oven
  Chemical Extraction:
    Do I get all of the RAS?
  Ignition oven:
    Do I burn off other organic matter?
AASHTO – Must use chemical extraction
Virginia – Developed ignition oven correction factor

## Slide 12: Asphalt Content Testing
Product | Average Ignition AC, % | Average TCE Extraction AC, % | Difference, %
WI – RAS | 30.75 | 25.77 | 4.98
AL – RAS | 22.77 | 18.92 | 3.85
TN – RAS | 18.77 | 17.73 | 1.04
NC – PC RAS | 18.64 | 16.84 | 1.8

## Slide 13: Deleterious Materials
Example specification (TEX-217-F Part III)
  Oven dry sample
  Sample 1000 g = WT
  Weigh Pan and pour sample over pan
  Magnet on pan catches metal pieces in shingle
  Weigh metal pieces = M

## Slide 14: Deleterious Materials
Sieves Used: 3/8”, No. 4, No. 8, No. 30
Shake sample for 10 minutes
Discard – No. 30 material
Test material retained on each sieve for deleterious materials (wood, paper, plastic, felt paper)
  Manual separation
Weigh material removed from RAS for each sieve
  Deleterious materials on 3/8” sieve =N3/8

## Slide 15: Deleterious Materials
P = percent of deleterious matter by weight
M = weight of material retained by magnet, g
N# = weight of deleterious substance on sieve, g

## Slide 16: Limits
Texas < 1.5%
Colorado (500-700 gram sample)
  Metals, rubber, glass, soil, brick < 3.0% on No. 4
  Paper, wood, plastic < 1.5% on No. 4

## Slide 17: Mix Design

## Slide 18: Shingle Binder Contribution
Organization | How Much RAS Binder Is Available for Mix?
AASHTO | Shingle Binder Availability
Alabama Department of Transportation | 100 of RAS binder
Iowa Department of Transportation | 66.7 percent of RAS binder
Missouri Department of Transportation | 100 Percent of RAS Binder
Texas Department of Transportation | 100 Percent of RAS Binder
Oregon Department of Transportation | 100 Percent of RAS Binder
What’s the truth?

## Slide 19: What Can Affect Binder Availability?
Size of RAS
Where is the RAS introduced
Aggregate temperature
Binder temperature
Mixing time
Moisture content!
Schroer 2009

## Slide 20: AASHTO Methodology
Perform volumetric mix design on a mix which contains all components but RAS
Perform a second mix design on a RAS mixture
  RAS added at ambient temperature to aggregate
    Should I heat the RAS overnight at 140F and then preheat for two hours at mix temp?
Determine the difference between the optimum asphalt content of virgin and RAS mixtures, Δ

## Slide 21: AASHTO Methodology
If Δ is positive, RAS is contributing binder
Multiply the percentage of shingle binder in the RAS by the percent RAS in the mix = total available binder
Divide Δ by total binder available
Correct shingle asphalt binder availability factor

## Slide 22: Limitations of Methodology
Assumes
  Differences in virgin and RAS mix is only due to shingle binder and not
    Fibers
    Aggregate
Townsend et al., 2007

## Slide 23: Current Methods
AASHTO – Choose a value for binder availability
Other states – Design for lower air voids to increase asphalt content
It’s all about the asphalt

## Slide 24: The Same, But Different

## Slide 25: The Same, But Different
Schroer 2009

## Slide 26: Melting Characteristics of RAS
Differential scanning calorimetry

## Slide 27: Shingle Gradation
Oversized shingles affect
  Asphalt mobilized
  Mixture consistency
State | Percent Passing |  |  |  | 
 | ½” | 3/8” | #4 | No. 100 | No. 200
Texas | 100% | 95% | -- | -- | --
Missouri | -- | 100% | -- | -- | --
GA/VA/AASHTO | -- | 100% | -- | -- | --
Iowa | 100% | 98% | 90% | -- | --
Oregon | 100% | 90% | -- | -- | --
South Carolina | 100% | -- | 70.0 – 95.0% | 15% Max | 7% Max
Minnesota | 100% | -- | 90% | -- | --

## Slide 28: Mix Design Must Be Tied to Performance
Performance Tests are going to be necessary as we move to more complicated mixtures
9-55
  Tie laboratory performance to field performance
  5 field projects
  Cracking Tests (Intermediate Temperature)
    Energy Ratio, Beam Fatigue, SCB (LTRC), SCB (IL), Overlay Tester,

## Slide 29: Field performance

## Slide 30: Can RAS Perform in a Mix?
YES!
But …

## Slide 31: Field Performance Methods
Randomly select three 200-ft sections for each mix
  Rutting – Straight edge and wedge
  Cracking – Visual Inspection and LTPP DIM
  Raveling – ASTM E965

## Slide 32: New Project #1
Appleton, Wisconsin
  September 10-12, 2013
  Mix design
    3% PC RAS, 14% RAP
    RAS Binder Ratio: 11.2%
    RAP Binder Ratio: 12.1%
  Mix iterations
    Control HMA, Zycotherm WMA, Rediset LQ WMA

## Slide 33: New Project #1
October 10, 2014
  13 months after construction
Rut depths measured with straight edge and wedge
  No rutting
Cracking assessment
  No cracking in Rediset mixture
  All concrete had been rubbilized before placing asphalt

## Slide 34: New Project #1 Cracking
Control Mixture
  One of three sections exhibited cracking
  Asphalt placed over concrete which had not been rubblized
  When placed over rubblized concrete, no cracking detected

## Slide 35: New Project #1 Cracking
Zycotherm Mixture
  One section exhibited cracking
  Asphalt placed over concrete which had not been rubblized
  Cracks lined up with joints

## Slide 36: New Project #1: Raveling
Mix | Mean Texture Depth, mm | Standard Deviation, mm
Control | 0.386 | 0.024
Rediset | 0.389 | 0.041
Zycotherm | 0.373 | 0.001
Pop-outs are commonly seen in this area.

## Slide 37: Field Projects
New Project #2 – Enterprise, AL
June 2014
Four mixtures
  RAP Binder Ratio: 13.5%
  RAS Binder Ratio: 19.6%
  Variables: Air Voids

## Slide 38: Performance
1st Revisit: 11/19/15
  All four test sections look good
  One small crack in low air void HMA test section

## Slide 39: Field Projects
New Project #3 – Tennessee
October 2014
Two mixtures
  RAP Binder Ratio: 10.9%
  RAS Binder Ratio: 11.7%
  Variable: HMA vs WMA

## Slide 40: Performance
1st Revisit: 11/11/15
Both mixtures look good
No cracking in either test section

## Slide 41: The Next Steps
While asphalt IS the most expensive mixture component, it is also critical for durability
Change our mindset to ensure performance
  Move away from binder tests
  Move towards mixture tests
  Ensure placing mixture in a place where it will succeed
  Rejuvenators

## Slide 42: Thank you!
J. Richard Willis
(334) 844-7301
willi59@auburn.edu