## Slide 1: ALDOT Updates
Scott George, P. E.
State Materials and Tests Engineer
2023 AAPA Conference
Auburn, AL
March 9, 2023

## Slide 2: ALDOT Specifications Updates Etc.
22GA008
OGFC Mix Design
BMD Validation/Verification

## Slide 3: 22GA0008
Subarticle 106.09(b)
Compaction on projects <1000 ft.
Items 106.09(c) 4. & 5.
Language changes regarding specific gravity
Notes: Added note after Table 1 that contractor shall use nuclear gauge to establish roller pattern that will achieve max. density.
Made edits to clarify the use of individual bulk specific gravity and max. specific gravity.

## Slide 4: 22GA0008
Subarticle 401.01(b)
Bituminous Treatment Table
Prime Coat
Article 410.01
WMA
Notes: Modified the prime coat placement rates, 0.10 – 0.25, and added a note stating that the engineer will set the rate within the limits in the table.
Expanded the use of WMA technology to Section 420 and Section 423 mixes

## Slide 5: 22GA0008
Subarticle 410.03(c)
Compaction for leveling
Subarticle 420.02(e)
PG Asphalt for Trackless Tack
Notes: Leveling shall be compacted in accordance with Subarticle 410.03(g). Contractor shall establish a rolling pattern using nuclear gauge to produce max. density. Deleted to the satisfaction of the engineer.
Added the approved PG asphalt for trackless tack products.

## Slide 6: 22GA0008
Subarticles 423.02(c) & 424.02(c)
Allowable Carbonate Stone Criteria
Notes: Disallows any sources with BPN9 values ≤ 20 can’t be used in surface mixes.

## Slide 7: 22GA0008
Article 804.07
Tables of Asphalt Materials
Notes: Updated dynamic shear and phase angles in the PG tables to be inline with most recent AASHTO requirements in M320.
Made a correction in Table 5 for the penetration requirement for HTSQ-1HL.

## Slide 8: OGFC Mix Design
  The procedure is very similar to the ASTM OGFC Design Procedure
  Contractors will set the AC%, not ALDOT
  There are new testing requirements to improve OGFC durability:
  Freeze-thaw
  Cantabro
  Dry Rodded Unit weight of aggregate blend
Notes: ASTM D 7064
Need projects to use the procedure.
Dry unit weight is an indicator of stone on stone contact.

## Slide 9: BMD Validation
STPAA-0055(519) AL 55 in Covington Co.
Need to validate the rutting and cracking values in our job special
Notes: April 28th is the let date
6 1000 ft. test sections with different rutting and cracking test targets
1000 ft control for standard 424A
approximately 750 tons of test mix on the road and allowing for 250 tons of possible trial mix
Rutting test HT-IDT
Cracking Test AL-CT based on IDEALCT
NCHRP 10-107 Guide for Implementing Balanced Mix Design Specifications

## Slide 10: Questions