## Slide 1: Spec Update 2026 AAPA Conference Tuscaloosa, AL March 11th & 12th
Chance Armstead, P.E.
ALDOT State Testing Engineer

## Slide 2: Section 106
106.09 (b) Added Note regarding density requirements for very short length pavement
Table 1
  Removed shutdown criteria tied to mix gradation
Notes: Note: For asphalt paving jobs that are 1000 feet or less in length, such as those at bridge or culvert replacements, the Contractor, as part of his QC plan, shall establish a rolling pattern using the nondestructive testing devices approved in Section 306 of the Specifications. The device shall either be calibrated to roadway cores or gage counts and shall be used to determine the rolling pattern producing maximum density. Contractor QC personnel shall be on site throughout each day to perform periodic checks and verify that the rolling pattern continually produces the maximum density that is achievable.

## Slide 3: Section 106 cont’d
Table 1
  Added Section 327 Plant Mix Bituminous Base requirements
  Removed TSR requirement during production
  Removed the Split Tensile Test
Notes: The previous Table 1 had no requirements for Section 327 Black Base requirements. There were only Section 327 PATB requirements
According to NAPA the TSR test is a good test for mix design but is a poor test for QA during production due to the test is time consuming. People usually like for production tests to be fast.
AASHTO T283
Says:
sample, compact, measure air voids.
Then half of the specimens need to be conditioned by:
Vacuum saturation, takes 20+ minutes per sample
Frozen for 16 hours minimum
Conditioned in 140°F water for 24 ± 1 hr
Conditioned at 77°F for 2 hours
And finally tested.
So, by the AASHTO method if I sample on Monday, I will not have a test result until Wednesday.
We have the Bituminous Lab working overtime, Saturdays & Sundays, getting JMF approval done b/c we are putting the mixes up with the anti-strip additives.
I don’t’ remember why we got rid of the split tensile test for 424 mixes

## Slide 4: Section 106 cont’d
Added language requiring “individual bulk specific gravity” to be used in calculations.
Add language that requires referee samples to be submitted to the central lab within 7 days after close of a lot.

## Slide 5: Section 106 cont’d
Bureau has 7 days to report results of the referee tests.
The contractor shall be notified within 24 hours that a referee sample is needed.
If these time constrains are not met, then the mix will be accepted on contractor testing.

## Slide 6: Section 327
Job mix may be designed by Marshall Method or a 60 gyratory compactor design.
Added a minimum stability for gyratory designs.
Added design air voids 4%.
Field density requirements to be handled by Table IV in section 410.08.
Notes: 2700 lbs. stability for 60 gyration designs. 1200 lbs. stability for 50 blow Marshall designs.
Density same as Superpave Mixes.

## Slide 7: Section 401
Modified prime treatment rates
Added language that the Engineer will set the rate within this range
401.03(b)1-Deleted the seasonal restrictions
Notes: New rates 0.10 to 0.25 gal/SY. Old rates 0.22 to 0.25 gal/SY.
Placement is now governed by weather alone. N. AL from Oct 1-May 1, S AL from Nov 1-April1; temperature requirements and roadway condition (wet) still apply

## Slide 8: Section 410
Contractor may use warm mix technology for all 423 & 424 mixes.
Anti-strip additives are required in all ALDOT mixes.

## Slide 9: Section 410 cont’d
Leveling will be compacted according to procedure in 410.03(g).
Smoothness requirement is only on final wearing layer.
Added 327 Plant Mix Bituminous Base Mixes to Table II
Notes: Use nuclear gauges to determine rolling pattern.
Deleted Table that implied that the layer under an OGFC also had to be tested for smoothness. That’s still a good idea but not for pay factors.
Table II are the pay factors for AC content and Voids in Total Mix

## Slide 10: Section 410 cont’d
Table IV- Target density shall be 94.0 % of the theoretical maximum density for all mixes except for: - the range of placement rates given in Item 306.03(g)3 (140 pounds per square yard or greater {76 kg per square meter or greater} and less than 200 pounds per square yard {109 kg per square meter} over surface treatments) the target density shall be 92.0 %.
Notes: 306.03(g)-States “A reduced density requirement will be allowed for layers…”, Table IV states “shall be”

## Slide 11: Section 410 cont’d
Table IV- Target density shall be 94.0 % of the theoretical maximum density for all mixes except for: - the range of placement rates given in Item 306.03(g)3 (140 pounds per square yard or greater {76 kg per square meter or greater} and less than 200 pounds per square yard {109 kg per square meter} over surface treatments) the target density shall be 92.0 %. The Contractor may request in writing that the target density remain 94% of the theoretical maximum density in these instances. Regardless of the target density, pay factors will be applied.
Notes: 306.03(g)-reduction will be allowed, Table IV states “shall be”

## Slide 12: Section 420
Added the 3 allowable “PG Asphalt for Trackless Tack” products.
Notes: Call them out by name.

## Slide 13: Sections 423 & 424
Updated the Allowable Carbonate Stone Requirements Table
Notes: To match what is in Section 450 for PCC pavement. The change was to not allow any carbonate stone with a BPN value less than or equal to 20.

## Slide 14: Future Updates
106.09(c)6-Delete density language
Section 403-Adding CSS-1EP for high polymer micro
Section 432- adding alternate for HDMB
Notes: “Pay factors above 1.00 will not be applied to mixes where the roadway density has been lowered below 94.0%”
403 Micro-surfacing
432-high density mineral bond

## Slide 15: Questions?