## Slide 1
Maximizing Joint Density

## Slide 2: Overview
Longitudinal Joint Density
Why does poor joint density occur at the longitudinal joint and optimal joint construction
Emerging Technologies
Overview of technologies past and present for achieving higher density figures
Maximizing Density Figures During The Paving Process
Real world examples using latest technologies during paving process
Questions
Achieving results during paving when numbers can be most gained

## Slide 3: Why Does Joint Density Matter?

## Slide 4: QUALITY
Why Does Joint Density Matter?
SAFETY
LIFECYCLE

## Slide 5: Why Does Joint Density Matter?
Technical Paper T-130: Longitudinal Joints Problems and Solutions

## Slide 6: Joint Density Specifications In America
No consensus on joint density specifications
Examples of States with detailed specifications
include:
  Michigan DOT: Allowance of vertical joints or tapered overlapping joints of 1:12. Average density must be ≥89% of Gmm, with incentives awarded for values above 90.50%
  Illinois DOT: Notch wedge joint, between 9” to 12” wide and roller attaching weighing 50 psi of width and equal to width of wedge (Fig. 1). Joint then coated with sprayed sealant
  Georgia DOT: tack the face of the open joint prior to placing adjoining mat.

## Slide 7: Joint Density Specifications In Tennessee
Joint Density Incentive/Disincentive |  | 
%Gmm |  | $/L.F./Lot
Min | Max | 
98.0 | 100 | *
97.0 | <98 | -0.70
96.0 | <97 | -0.42
95.0 | <96 | 0.00
94.0 | <95 | 0.00
93.0 | <94 | 0.07
92.0 | <93 | 0.14
91.0 | <92 | 0.07
90.0 | <91 | 0.00
89.0 | <90 | -0.14
88.0 | <89 | -0.42
87.0 | <88 | -0.70
 | <87 | -0.98
 | <86 | *
SP407DEN: Special Provision Regarding Bituminous Plan Mix Pavements (Hot Mix) Roadway Density (Rev. 4-15-19)
Tennessee has recently begun implementing density
incentive/disincentive for joint density
5 selected cores from each lot to be tested for density compliance and acceptance in accordance to AASHTO T-166 Method A only (Suspension)
No specification of the devices or technologies to be used.
  Speaks mostly to compaction

## Slide 8: Joint Construction Technologies
How do we create a better constructed longitudinal
joint to:
  Create longer lasting roadways;
  Achieve DOT specifications for joint density;

## Slide 9: Eliminating Joint Density
No Joint
Echelon
These paving methods not possible on most projects!

## Slide 10: Pre- & Post-Paving Technologies
Cutting Back Edge
Joint Heater
Longitudinal Joint Sealing
Advantages
Create strong bond through adhesion at a cold joint
Lower permeability at the joint
Drawbacks
Expensive specialized equipment and training
Little data to support improving joint density
Insufficient data on long term lifecycle
Advantages
Cut back lowest density portion of the mat for higher density at the outside edge
Leaves vertical joint for second pass
Drawbacks
Wasted material = financial impact
Steering the roller cutter is challenging
Clean up of cut away material is costly
Advantages
Reheating of the cold joint allowing mix from second pass to be rolled into the softened areas
Drawbacks
Slower pave speeds/lower production
Specialized knowledge in set up and operation
Fueling of heating apparatus and track delamination

## Slide 11: Technologies
GOOD
BETTER
BEST
Michigan Joint/Tapered Notch
Extrusion & Edge Compaction
Technologies During The Paving
Process Into 3 Categories:

## Slide 12: Edge Compaction
Edge Compaction simply means containing the
material on both sides of the first pass.
Create more uniform density across width of the screed while achieving a vertical joint for second pass
Can be achieved by using:
  Standard heated endgate
  Safety Edge Device
  Roller Mounted Wheel for cutting back

## Slide 13: Edge Compaction

## Slide 14: Edge Compaction
- Density across mat with endgate up and no compaction/containment

## Slide 15: Edge Compaction
-Density across mat with endgate aiding edge compaction/containment

## Slide 16: Edge Compaction
Safety Edge Device
Edge Compression Device

## Slide 17: Michigan Joint
Edge Compaction simply means containing the
material on both sides of first pass
Create more uniform density across width of the screed while achieving a vertical joint for second pass
Containing open edge with wedge of material to prevent shoving under compactive effort

## Slide 18: Michigan Joint

## Slide 19: Michigan Joint
1 – Density on the first pass showing at the taper and partial edge compaction
2 – Density across mat on
second overlapping pass

## Slide 20: Combination
Combining the concepts of edge compaction with
material extrusion to create higher joint density
Increasing density at the outside edge
Can be achieved by using:
  Standard heated endgate
  Sideload endgate runner

## Slide 21: Combination

## Slide 22: Combination
1 – Density on the first pass showing additional density under 4” and edge containment

## Slide 23: Combination
2 – Density across mat with second pass showing high concentration of dense material at the joint

## Slide 24: Combination - Tennessee
Thickness (in.) | Theoretical Density | Marshall Density
2.459 | 93.5% | 96.6%
2.247 | 93.7% | 96.8%
2.246 | 94.5% | 97.7%
2.029 | 93.3% | 96.2%
2.176 | 93.8% | 96.8%
1.891 | 93.8% | 96.8%
2.034 | 94.4% | 97.4%
2.001 | 93.1% | 96.2%
2.026 | 94.6% | 97.8%
2.079 | 93.8% | 97.0%
2.112 | 93.2% | 96.4%
2.035 | 93.7% | 96.9%
2.004 | 92.7% | 95.9%
2.009 | 93.3% | 96.1%
2.036 | 93.0% | 95.8%
2.061 | 93.1% | 95.9%
2.169 | 92.9% | 96.1%
2.181 | 93.4% | 96.6%
2.266 | 94.0% | 97.3%
2.058 | 94.0% | 97.2%
2.167 | 93.3% | 96.4%
2.291 | 93.8% | 97.0%
2.203 | 93.3% | 96.4%
2.091 | 93.7% | 96.8%
96.7% Marshall Density Average

## Slide 25: Combination - Tennessee
Joint Tracking Device
Ensures proper overlap at the vertical joint for optimum joint density
Takes the human element out = more efficient results

## Slide 26: Conclusion
Longitudinal joint density will continue to be front and center in the industry’s pursuit of longer lasting, safer roadways
With the emerging technologies during the paving process, creating more impervious, dense joints both economical and operator friendly

## Slide 27: Questions