## Slide 1: Buzz and Dave
and Dave

## Slide 3: Four Installments to Date
Winter ‘243 – skipping tack, RAM cooling, ≤4 x NMAS
Spring ‘253 – coefficients, thick perpetual, lean binder
Summer ‘254 – big rock, low Va, friction agg, COAC
Fall ‘254 – fogging OGFC, complexity, ’93 Guide, PTRs.

## Slide 4
Do you have access to Asphalt Magazine articles?

## Slide 5: www.HeyNAPA.com
“I don't have direct access to external publications, including articles from Asphalt Magazine. However, I can provide information and answer questions related to asphalt paving, materials, and industry practices. If there's a specific topic or question you have in mind, please let me know, and I'll be happy to assist you with the information I have!”

## Slide 6
NCAT Pavement Test Track

## Slide 7: Four Installments to Date
Winter ‘243 – skipping tack, RAM cooling, 4xNMAS
Spring ‘253 – coefficients, thick perpetual, lean binder
Summer ‘254 – big rock, low Va, friction agg, COAC
Fall ‘254 – fogging OGFC, complexity, ’93 Guide, PTRs.

## Slide 8: Winter 2024
Paving thicker than 4 times NMAS hurts compaction
Higher recycled asphalt mix (RAM) cools faster
Tack coat can be skipped between multiple lifts.

## Slide 9
What are the upper & lower limits on paving thicknesses?

## Slide 10: HeyNAPA.com
Fine mix lifts should be placed 3 to 5 x NMAS
Coarse mix lifts should be placed 4 to 6 x NMAS
Justification is ability to compact & measure smooth
“Thick lifts” are greater than 5fine and 6coarse x NMAS
½” mixes are “thick lift” when > 2½”fine and 3”coarse
3 Track sections2018 have ratios between 14 & 16!

## Slide 11: Tack Coat
Purpose of Each Layer | N5 Control | S5 Higher RAP | S6 RAP+RAS | S13 Recyc Tires
Durable, Rut Resistant Surface | 20% RAP20 67-22/82-16 DG | 25% RAP11 67-22/76-22 SMA | 5% RAS21 67-22/88-16 SMA | VIRGIN 82-2212 SMA
Stiff, Strain Reducing Middle | 35% RAP39 67-22/88-10 DG | 50% RAP41 67-22/82-16 DG | 50% AGED26-24 67-22/94-10 DG | 35% RAP37 82-2212 DG
Fatigue Resistant Base Layer | 35% RAP39 67-22/88-10 DG | 35% RAP34 94-28/94-10 DG | 25% RAP24 +76-22/88-16 DG | VIRGIN 88-2220 AZ
Green = Evotherm Q1 Additive, Blue = Astec Green Foamer

## Slide 12: Spring 2025
Intermediate layer mixes can be leaner, stiffer
Layer coefficients should be the same for all mixes
Pavements must be very thick to be perpetual.

## Slide 13: Thin Perpetual Pavements
5¾”

## Slide 14: NCAT Report 25-01
x 1.7 !

## Slide 15: Summer 2025
Big rocks are necessary for strong (lower) asphalt
Polishing sources should be banned from surface mix
RBA implementation requires changing volumetrics
Low Va & high VFA always risks rutting & bleeding.

## Slide 16: Friction and Safety

## Slide 17: Low Void “HiMod” Mixes in Utah
Higher Density (~97% on 46 projects)
Better binder (≥5% polymer)
More binder (typically +20%)
15% RAP (sustainable).

## Slide 18: Low Void “HiMod” Mixes in Utah
Bridge decks, rubblization overlays, SMA swaps
3” for interstate bridge deck preservation
5½“ on rubblization ($40M savings vs PCC rebuild!)
PCC advocate now flipping projects for cost savings
Up to 7” in a single lift in specialty applications
2” as switch from SMA standard overlay (less cost)
More expensive than DGA, less than SMA.

## Slide 19: Fall 2025
Pavements designed thinner than ’93 Guide will fail
More complex specs are needed to improve quality
Rubber-tired rollers (PTRs) are not worth the cost
Fogging OGFC surfaces will reduce permeability.

## Slide 20: 2000 NCAT Pavement Test Track
24”

## Slide 21: 2003 NCAT Pavement Test Track
9”

## Slide 22: 2009 NCAT Pavement Test Track
5¾”

## Slide 23: Simple BMD for AL Counties
https://www.ncat.us
Publications
NCAT Newsletter
Spring 2021
Volume 33
Number 1
Page 6.

## Slide 24: Mix Busters Big Takeaways
Better tack or elimination via thicklay paving
Higher layer coefficients from innovation
Perpetual asphalt at concrete thickness
BMD for Vbeff quantity and quality
Specify performance with less words
1) Protect taxpayers and 2) incentivize innovation
Cracking, rutting, friction at lowest $/C BMD+f, LCA
Requests: asphaltmixbuster@gmail.com

## Slide 25: #BuzzOnAsphalt
#DriveAsphalt