## Slide 1
NCAT Test Track Update
Nathan Moore, P.E.
2026 AAPA Conference
March 12, 2026

## Slide 2: 2024-2027 NCAT Test Track Sponsors

## Slide 3: Appreciation and Thanks!
Asphalt Plus
Asphalt Solutions
Associated Asphalt
Astec
Aztec Asphalt Technology
Blacklidge
C.W. Matthews
Cargill
CAT
Chris Clark Grading and Paving
Cimline
Collaborative Aggregates
Corrective Asphalt Materials
East Alabama Paving
Ergon Asphalt and Emulsions
Great Lakes Minerals
Hi-Tech Asphalt Solutions
Ingevity
JAG Trucking
Jon Grelle
Larry Scofield/IGGA
Lehigh
Liberty Tire
Pavement Resoration Inc.
Russell Standard
Skidabrader
Southeast Grinding & Grooving
Tractor Equipment Company
Wirtgen/Hamm
Vulcan Materials

## Slide 4
2024 Track Build by the Numbers
58 unique aggregate/RAP stockpiles
>300 truck loads of aggregate/RAP hauled in
6 different asphalt binders + 3 tack products + 1 VRAM
4 asphalt plants (2 HMA + 1 Wirtgen KMA + 1 PRI Pugmill)
30 unique mixes + 31 trial runs (practice runs)
3 CCPR + 23 HMA + 4 WMA mixes
16 actively instrumented structural test sections
2 sections removed and replaced

## Slide 5
2024 Track Build by the Numbers
36 working days (7 weeks + 1 day)
2 hurricane delays (Helene & Milton)
  Delayed by only 3 days
850+ buckets of mix sampled
7 new NCAT personnel in critical roles during build process
75+ visitors during Track construction
Notes: NCAT people:
Nathan – Director
Zane, Graham, Madison – Lab engineers / mix designers
Robert – Lead Track technician
Mike – Trucking coordinator / plant QC/QA
Cody – Photography/videographer

## Slide 6
2024 Track Build by the Numbers (QC Results)
Parameter Avg Δ (Target – Actual)
  #4 Sieve - 0.8%
  #8 Sieve +0.6%
  #30 Sieve +0.2%
  #200 Sieve +0.3%
  Air Voids +0.1%
  VMA +0.1%
  Lift Thickness -0.03 in
Average Density 94.4%
Minimum Density 92.6%
Notes: NCAT people:
Nathan – Director
Zane, Graham, Madison – Lab engineers / mix designers
Robert – Lead Track technician
Mike – Trucking coordinator / plant QC/QA
Cody – Photography/videographer

## Slide 8: NCAT Test Track Research Cycle
Phase 1
Plan/Build Test Sections
Phase 2
Traffic
Phase 3
Forensic Analysis

## Slide 9: ALDOT Higher RAP + BMD (W8 & W9)

## Slide 10: ALDOT BMD Sections
“BMD for all stakeholders”
  Improved durability
  Allowance for more RAP and innovation
Higher RAP (35%) + softer binder
  W8 – PG 67-22 + Recycling Agent (3-in-1)
  W9 – PG 58-28
½” ALDOT 424 mix (+ 15% RAP)

## Slide 11: Materials and Mix Design
Granite 89s – 29%
Granite M10s – 17%
Sand – 19%
RAP – 35%
AC – 6.0%
Liquid additives:
W8 (Evo CA-17) – 2.5%
W9 (Evo. P25) – 0.5%
W8
W9

## Slide 12: BMD Results (design)
Improving Rutting
Improving Cracking
Ndes = 60
Va% = 4.0%
VMA > 16

## Slide 13: Construction

## Slide 14: Production Results
W8
W9
Shifts slightly finer

## Slide 15: Notable QC/Acceptance Results
 | W8 (PG 67-22 + RA) | W9 (PG 58-28)
AC% | 6.1% | 6.1%
Air Voids, % | 2.6% | 2.3%
In-place Density, % | 94.1% | 93.6%
Thickness, in | 1.8” | 1.9”
Production Temp, °F | 305 °F | 305 °F

## Slide 16: BMD During Production Results

## Slide 17: Early Performance @ 6M ESALs
Less than 0.1 inches (3 mm) of rutting
No significant smoothness changes
Slight texture increase (binder films wearing off)
Investigating a couple of unexpected cracks

## Slide 18: Additives on the Test Track

## Slide 19: Dry Rubber ARGG (AR - N11)

## Slide 20: Surface Preparation Plan
Notes: ARDOT looking for a crack-resistant surface layer to delay reflective cracks from poorly rubblized PCC.

## Slide 21: Dry Rubber – Liberty Tire
Smart Mix is a pre-swelled rubber with extender oil
Added at 20% by weight of virgin binder

## Slide 22: ARGG Mix Design
UTBWC Gradation (Gap-graded)
PG 70-22
Virgin Mix
5.9% AC + 1.2% Rubber

## Slide 23: Sawcut performance @ ~2M ESALs
Dry ARGG Section
Other Sawcut Section

## Slide 24: Smoothness Changes
Sawcut BMD sections with 58-28 binder
ARDOT Gap-Graded Dry Rubber Mix

## Slide 25: Sawcut performance @ 5M ESALs
Other Sawcut Section

## Slide 26: Other Additive* Examples
Catalloy Polymer

## Slide 27: Other Additive* Examples
Bauxite in Thin Overlay

## Slide 28: Other Additive* Examples
WMA + Rejuvenator
Dry Rubber in DGA/SMA
HP Binder

## Slide 29: Additive Group Experiment

## Slide 33
eng.auburn.edu/the-nextpave-challenge/

## Slide 35
Thank you!!
Nathan Moore, P.E. nathanmoore@auburn.edu